Product type:

Fully biodegradable blown film grade resin（Ingredients：PBAT,PLA,CaCO3)

Characteristics:

M-2005 is a fully biodegradable material with high  tensile. The main  component is a fully biodegradable polymer

blends with polylactic acid (PLA) and inorganic filler. The film products have excellent mechanical property.

After 180 days under composting conditions, it can be completely biodegraded into water,Carbon dioxide and non- toxic minerals have no pollution to the environment.

Applications:

It is mainly applicable to blow molding  processing of film products, typical products include but  not limited to supermarket shopping bags, courier bags, clothing bags, industrial package,etc.

Process equipment:

It is suggested that each heating section of the extruder is gradually increased from 145℃ to 155℃. The temperature for headpiece should be controlled at around 155-160℃. It can be properly adjusted according to the conditions of each blowing machine.

The film blow-up ratio can be adjusted according to the demand of the film thickness.(Preferably around 2.5-3

LDPE blowing machine is applicable(high pressure die), length-diameter ratio of film blowing machine should be ≥ 30.

Product certifications:

Compliant with European EN 13432 , passed European DINCERTCO compost product certification

Package&storage:

25KG/bag or customized according to customer requirements.

It should be stored in a dry and cool place, pay attention to moisture, keep the packaging intact and prevent damage.

It can be used directly after opening the package, and the unused packaging must be sealed and stored. If the package is opened for a long time, it should be dried before use; the drying condition is 60ºC for 4 hours; or 90°C for 1 hour in a blast oven. If the machine is shut down for a long time during the processing, the tail material in the barrel needs to be eliminated to avoid degradation and discoloration of the material.

Product index:

| Index | Testing standard | Unit | Value |
| --- | --- | --- | --- |
| Appearance | Visually | —— | Translucent/transparent granules |
| Density | ISO 1183 | g/cm3 | 1.35±0.02 |
| MFR （190℃ 2kg) | ISO 1133 | g/10min | ≦5 |
| Hardness | ASTM-D2240 | D | 50-60 |
| Melting temperature | ISO3146 | ℃ | 95-155 |
| Thermal decomposition temperature | ASTM-D6370 | ℃ | 370 |

Contacts:

Company: Hangzhou Peijin Chemical Co., Ltd.

Add: Floor 7th, No.332, Xihua street, Hangzhou, Zhejiang, China P.C.310012

Tel: +86-571-86333092

Fax: +86-571-86333092

E-mail: amylin@pekinchem.com